## Slide 1
Introduction to Composite Materials (Laminated Composite Materials)
Mechanical Engineering Instructor: Autar Kaw

## Slide 2: 2007 Titus Racer X Exogrid

## Slide 3: The Full Page Ad for 2007 Titus Racer X Exogrid

## Slide 4: My wish

## Slide 5: What are you going to learn?
What are composite materials?
How are they manufactured?
What advantages and drawbacks do composites have over metals?
Develop mathematical models to understand the mechanical response of composites to mechanical and hygrothermal loads?
Use the above mathematical models to optimally design structures made of composites.

## Slide 6: What is a composite?
A composite is a structural material which consists of combining two or more constituents
Examples:
  Flesh in your leg reinforced with bones
  Concrete reinforced with steel
  Epoxy reinforced with graphite fibers.

## Slide 7
“You are no longer to supply the people with straw for making bricks; let them go and gather their own straw” - Exodus 5.7.

## Slide 8: Shift in Paradigm About Materials
“More important than any one new application is the new ‘materials’ concept itself ”
Peter F. Drucker
The Age of Discontinuity, 1969

## Slide 9: What is this paradigm shift in materials?
From substance to structures
From artisan to science
From workshop to mathematical modeling
From what nature provides to what man can accomplish

## Slide 10: From constituents to application

## Slide 11: Chapter 1 Introduction to Composite Materials

## Slide 12: Short Videos on Composite Materials
Some videos of composite materials
NASA uses composite materials in shuttle
Composites improve efficiency
Cloth composites

## Slide 13: Chapter 1: Objectives
What is a composite?
What are the advantages and drawbacks of composites over monolithic materials?
What factors influence mechanical properties of a composite

## Slide 14: Chapter Objectives (continued)
How do we classify composites?
What are the common types of fibers and matrices?
How are composite materials manufactured?
What are the mechanical properties of composite materials?

## Slide 15: Chapter Objectives (continued)
Give applications of composite materials.
How are composites recycled?
What terminology is used for studying mechanics of composites?

## Slide 16: What is an advanced composite?
Advanced composites are composite materials which were traditionally used in aerospace industries
Examples include graphite/epoxy, Kevlar/epoxy and Boron/aluminum

## Slide 17: Examples of Natural Composites
Wood
  Cellulose Fibers
  Lignin Matrix
Bones
  Collagen Fibers
  Mineral Matrix

## Slide 18: Why composites over metals?
High Strength and High Stiffness
Tailored Design
Fatigue Life
Dimensional Stability
Corrosion Resistance

## Slide 19: Why Composites over Metals?
How is the mechanical advantage of composite measured?

## Slide 20: Specific Strength vs. Year

## Slide 21: Table 1.1. Specific modulus and strength of typical fibers, composites and bulk metals

## Slide 22: Comparative Thermal Expansion Coefficients (μin/in/oF)
Material | Direction-x | Direction-y
Steel | 6.5 | 6.5
Aluminum | 12.8 | 12.8
Graphite | -0.02 | 1.1
Unidirectional Graphite/Epoxy | 0.01 | 12.5
Cross-Ply Graphite/Epoxy | 0.84 | 0.84
Quasi-Isotropic Graphite/Epoxy | 0.84 | 0.84

## Slide 23: Specific Strength vs Specific Modulus

## Slide 24: Other Mechanical Parameters
Are specific modulus and specific strength the only mechanical parameters used for measuring the relative advantage of composites over metals? NO!!

## Slide 25: Tailored Design
Engineered to meet specific demands as choices of making the material are many more as compared to metals.
Examples of choices
  fiber volume fraction
  layer orientation
  type of layer
  layer stacking sequence

## Slide 26: Fatigue Life
Fatigue life is higher than metals such as aluminum.
Important consideration in applications such as
  aircrafts
  bridges
  structures exposed to wind

## Slide 27: Dimensional Stability
Temperature changes can result
  in overheating of components (example engines)
  thermal fatigue due to cyclic temperature changes (space structures)
  render structures inoperable (space antennas)

## Slide 28: Corrosion Resistance
Polymers and ceramics matrix are corrosion resistant
Examples include
  underground storage tanks
  doors
  window frames
  structural members of offshore drilling platforms

## Slide 29: What is most limiting factor in the use of composites in structures?
Lack of engineers with the knowledge and experience to design with these materials!!!!

## Slide 30: Cost Considerations
Composites may be more expensive per pound than conventional materials. Then why do we use composite materials?

## Slide 31: Factors in Cost Estimate
For Composite Materials
  Fewer pounds are required
  Fabrication cost may be lower
  Transportation costs are generally lower
  Less maintenance than conventional materials is required

## Slide 32: Fiber Factors
What fiber factors contribute to the mechanical performance of a composite?
    Length
    Orientation
    Shape
    Material

## Slide 33: Fiber Factor - Length
Long Fibers
  Easy to orient
  Easy to process
  Higher impact resistance
  Dimensional stability
Short Fibers
  Low Cost
  Fast cycle time

## Slide 34: Fiber Factor - Orientation
One direction orientation
  High stiffness and strength in that direction
  Low stiffness and strength in other directions
Multi-direction orientation
  Less stiffness but more direction independent

## Slide 35: Fiber Factor - Shape
Most common shape is circular
Hexagon and square shapes give high packing factors

## Slide 36: Fiber Factor - Material
Graphite and aramids have high strength and stiffness
Glass has low stiffness but cost less

## Slide 37: Matrix Factors
What are the matrix factors which contribute to the mechanical performance of composites?
  Binds fibers together
  Protects fibers from environment
  Shielding from damage due to handling
  Distributing the load to fibers.

## Slide 38: Factors Other Than Fiber and Matrix
Fiber-matrix interface
  Chemical bonding
  Mechanical bonding

## Slide 39: Fiber Types
Glass Fiber (first synthetic fiber)
Boron (first advanced fiber)
Carbon
Silicon Carbide

## Slide 40: Types of Matrices
Polymers
Metals
Ceramics

## Slide 41: Polymer Matrix
Thermosets
  polyester
  epoxy
  polymide
Thermoplastics
  polypropylene
  polyvinyl chloride
  nylon

## Slide 42: Metal Matrix
Aluminum
Titanium
Copper

## Slide 43: Ceramic Matrix
Carbon
Silicon Carbide
Calcium AluminoSilicate
Lithium AluminoSilicate

## Slide 44: Why do fibers have thin diameter?
Less flaws
More toughness and ductility
Higher flexibility
Thin Fiber
Thick Fiber

## Slide 45: Less Flaws

## Slide 46: More Toughness and Ductility
Fiber-matrix interface area is inversely proportional to the diameter of the fibers
Higher surface area of fiber-matrix interface results in higher ductility and toughness, and better transfer of loads.

## Slide 47: More Flexibility
Flexibility is proportional to inverse of
    Young’s modulus
    Fourth power of diameter
Thinner fibers hence have a higher flexibility and are easy to handle in manufacturing.

## Slide 48: END

## Slide 49: Fibrous Composites
Generally there are two phases
  Fiber as a reinforcement
  Matrix as a binder

## Slide 50: Historical Perspective
4000 B.C. Fibrous composites were used in Egypt in making laminated writing materials
1300 BC: Reference to Book of Exodus
1700 AD: French Scientist, Reumer talked about potential of glass fibers

## Slide 51: Historical Perspectives (continued)
1939: Glass fiber manufactured commercially for high temperature electrical applications
1950s: Boron and carbon fibers were produced to make ropes.
1960s: Matrix added to make polymeric matrix composites

## Slide 52: Historical Perspectives (continued)
1970s: Cold war forces development of metal matrix composites for military aircrafts and missile guidance systems
1990s: High temperature ceramic matrix composites are being aggressively researched for use in next generation aircraft engines and power plant turbines

## Slide 53: Shipments of Composites

## Slide 54: World Market of Composites

## Slide 55: Advantages of Composites
Specific Strength and Stiffness
Tailored Design
Fatigue Life
Dimensional Stability
Corrosion Resistance
Cost-Effective Fabrication

## Slide 56: Drawbacks of Composites
High cost of fabrication of composites
Complex mechanical characterization
Complicated repair of composite structures
High combination of all required properties may not be available

## Slide 57
END

## Slide 58: Composites vs. Metals

## Slide 59: Composites vs. Metals
Comparison based on six primary material selection parameters

## Slide 60: Design Parameters
Torque Resistance.
  Should carry load without failure
Not rotate close to natural frequency.
  Need high natural frequency otherwise whirling may take place
Buckling Resistance.
  May buckle before failing