## Slide 1
Classification of Composite Materials
Mechanical Engineering Instructor: Autar Kaw

## Slide 2: Classification
CONCRETE:
Gravel, sand and cement
PAINT:
Paint and aluminum flakes
GRAPHITE/EPOXY:
Graphite fibers in epoxy matrix

## Slide 3: Polymer Matrix Composites
What are the most common advanced composites?
  Graphite/Epoxy
  Kevlar/Epoxy
  Boron/Epoxy

## Slide 4: Polymer Matrix Composites
What are the drawbacks of polymer matrix composites?
  Low operating temperatures
  High CTE and CMEs
  Low elastic properties in certian directions

## Slide 5: Are Carbon and Graphite the Same?
No
  Carbon fibers have 93%-95% carbon content and graphite has >99% carbon content
  Carbon fibers are produced at 2400o F and graphite fibers are produced at 3400o F

## Slide 6: Table 1.4. Typical mechanical properties of polymer matrix composites and monolithic materials

## Slide 7: Comparative Stiffness of PMCs and Metals

## Slide 8: How to make a PMC

## Slide 9: Schematic of Prepreg Manufacturing

## Slide 10: Prepreg Boron/Epoxy

## Slide 11: Autoclave Lamination

## Slide 12: Filament Winding
Filament Winding Video

## Slide 13: Common PMC Fibers & Matrices
Fibers
  Graphite
  Glass
  Kevlar
Matrices
  Epoxy
  Phenolic
  Polyester

## Slide 14: Table 1.5 Typical mechanical properties of fibers used in polymer matrix composites

## Slide 15: Cost Comparison of PMC fibers
Type of fiber Cost ($ per pound)
A-glass 0.65 - .90
C-glass 0.75 - 1.00
E-glass 0.75 - 1.00
S-2 Glass 6.00 - 8.00
Heavy Tow 9.00 - 12.00
Medium Tow 15.00 -20.00
Low Tow 40.00 -70.00+
Kev29 12.00 -14.00
Kev149 25.00 -30.00

## Slide 16: Manufacturing of Glass Fibers

## Slide 17: Glass Fiber Types
E-glass (fiberglass) - electrical applications
S-glass - strength applications
C-glass - Corrosion resistant
D-glass - Low dielectric applications
A-glass - Appearance applications
AR-glass - Alkali resistant

## Slide 18: Table 1.6 Comparison of properties of E-glass and S-glass

## Slide 19: Table 1.7 Chemical Composition of E-Glass and S-Glass Fibers

## Slide 20: Fig 1.10 Forms of Fibers

## Slide 21: Fig 1.11 Manufacturing Graphite Fibers

## Slide 22: Resin Systems
Polyester
Phenolics
Epoxy
Silicone
Polymide

## Slide 23: Properties of epoxy

## Slide 24: Curing Stages of Epoxy

## Slide 25: Comparison of Resins

## Slide 26: Difference between thermosets and thermoplastics

## Slide 27: Pre-Preg Graphite/Epoxy