## Slide 1: EML 4230 Introduction to Composite Materials
Chapter 2 Macromechanical Analysis of a Lamina
Tsai-Wu Failure Theory
Dr. Autar Kaw
Department of Mechanical Engineering
University of South Florida, Tampa, FL 33620
Courtesy of the Textbook
Mechanics of Composite Materials by Kaw

## Slide 2: Tsai-Wu Failure Theory
Tsai-Wu applied the failure theory to a lamina in plane stress. A lamina is considered to be failed if:
is violated. This failure theory is more general than the Tsai-Hill failure theory because it distinguishes between the compressive and tensile strengths of a lamina.
The components H1 – H66 of the failure theory are found using the five strength parameters of a unidirectional lamina.
H1σ1+H2σ2+H6τ12+H11
+H22
+H66
+2H12σ1σ2< 1

## Slide 3: Components of Tsai-Wu Fail
to a unidirectional lamina, the lamina will fail. Equation
(2.152) reduces to:
a) Apply
to a unidirectional lamina, the lamina will fail. Equation
(2.152) reduces to:
b) Apply
From Equations (2.153) and (2.154),

## Slide 4: Components of Tsai-Wu Fail
to a unidirectional lamina, the lamina will fail. Equation
(2.152) reduces to
c) Apply
to a unidirectional lamina, the lamina will fail. Equation
(2.152) reduces to:
d) Apply
From Equations (2.157) and (2.158):

## Slide 5: Components of Tsai-Wu Fail
to a unidirectional lamina, the lamina will fail. Equation
(2.152) reduces to:
e) Apply
to a unidirectional lamina, the lamina will fail. Equation
(2.152) reduces to:
f) Apply
From Equations (2.157) and (2.158),

## Slide 6: Determination of
Apply equal tensile loads along the two material axes in a unidirectional composite. If
is the load at which the lamina fails, then:
The solution of the Equation (2.165) gives:

## Slide 7: Determination of
Take a 450 lamina under uniaxial tension
. The stress
at failure is noted.
If this stress is
then using Equation (2.94), the local stresses at failure are:
Substituting the above local stresses in Equation (2.152):

## Slide 8: Empirical Models of
as per Tsai-Hill failure theory8
as per Hoffman criterion10
as per Mises-Hencky criterion11

## Slide 9: Example 2.19
Find the maximum value of
if a stress
and
are applied to a 600 lamina of Graphite/Epoxy. Use Tsai-Wu failure theory. Use the properties of a unidirectional Graphite/Epoxy lamina from Table 2.1.

## Slide 10: Example 2.19
Using Equation (2.94), the stresses in the local axes are:

## Slide 11: Example 2.19
H12=

## Slide 12: Example 2.19
Substituting these values in Equation (2.152), we obtain:
or

## Slide 13: Example 2.19
If one uses the other two empirical criteria for H12 as per Equation (2.171), one obtains:
Summarizing the four failure theories for the same stress-state, the value of S obtained is:
S = 16.33 (Maximum Stress failure theory),
= 16.33 (Maximum Strain failure theory),
= 10.94 (Tsai-Hill failure theory),
= 16.06 (Modified Tsai-Hill failure theory),
= 22.39 (Tsai-Wu failure theory).

## Slide 14: END