## Slide 1: EML 4230 Introduction to Composite Materials
Chapter 3 Micromechanical Analysis of a Lamina
Volume Fractions, Weight Fractions,
Density, and Void Content
Dr. Autar Kaw
Department of Mechanical Engineering
University of South Florida, Tampa, FL 33620
Courtesy of the Textbook
Mechanics of Composite Materials by Kaw

## Slide 2: Volume Fractions

## Slide 3: Fiber Packing
FIGURE 3.9
Fiber to fiber spacing in (a) square packing geometry and (b) hexagonal packing geometry.

## Slide 4: Weight Fractions

## Slide 5: Volume and Weight Fractions

## Slide 6: Volume and Weight Fractions

## Slide 7: Volume and Weight Fractions

## Slide 8: Density

## Slide 9: Example
Example 3.1
A Glass/Epoxy lamina consists of a 70% fiber volume fraction. Use properties of glass and epoxy from Tables 3.1 and 3.2, respectively to determine the
density of lamina
b) mass fractions of the glass and epoxy
c) volume of composite lamina if the mass of the lamina is 4 kg.
d) volume and mass of glass and epoxy in part (c).

## Slide 10: Example
Property | Units | Graphite | Glass | Aramid
Axial modulus Transverse modulus Axial Poisson's ratio Transverse Poisson's ratio Axial shear modulus Axial coefficient of thermal expansion Transverse coefficient of thermal expansion Axial tensile strength Axial compressive strength Transverse tensile strength Transverse compressive strength Shear strength Specific gravity | GPa GPa - - - - - - GPa μm/m/0C μm/m/0C MPa MPa MPa MPa MPa - - - | 230 22 0.30 0.35 22 -1.3 7.0 2067 1999 77 42 36 1.8 | 85 85 0.20 0.20 35.42 5 5 1550 1550 1550 1550 35 2.5 | 124 8 0.36 0.37 3 -5.0 4.1 1379 276 7 7 21 1.4
Table 3.1 Typical Properties of Fibers (SI system of units)

## Slide 11: Example
Property | Units | Epoxy | Aluminum | Polyamide
Axial modulus Transverse modulus Axial Poisson's ratio Transverse Poisson's ratio Axial shear modulus Coefficient of thermal expansion Coefficient of moisture expansion Axial tensile strength Axial compressive strength Transverse tensile strength Transverse compressive strength Shear strength Specific gravity | GPa GPa - - - - - - GPa μm/m/0C m/m/kg/kg MPa MPa MPa MPa MPa - - - | 3.4 3.4 0.3 0.3 1.308 63 0.33 72 102 72 102 34 1.2 | 71 71 0.30 0.30 27 23 0.00 276 276 276 276 138 2.7 | 3.5 3.5 0.35 0.35 1.3 90 0.33 54 108 54 108 54 1.2
Table 3.2 Typical Properties of Matrices (SI system of units)

## Slide 12: Example
Property | Units | Graphite | Glass | Aramid
Axial Modulus Transverse modulus Axial Poisson's ratio Transverse Poisson's ratio Axial shear modulus Axial coefficient of thermal expansion Transverse coefficient of thermal expansion Axial tensile strength Axial compressive strength Transverse tensile strength Transverse compressive strength Shear strength Specific gravity | Msi Msi - - - - - - Msi μin/in/0F μin/in/0F ksi ksi ksi ksi ksi - - - | 33.35 3.19 0.30 0.35 3.19 -0.7222 3.889 299.7 289.8 11.16 6.09 5.22 1.8 | 12.33 12.33 0.20 0.20 5.136 2.778 2.778 224.8 224.8 224.8 224.8 5.08 2.5 | 17.98 1.16 0.36 0.37 0.435 -2.778 2.278 200.0 40.02 1.015 1.015 3.045 1.4
Table 3.3 Typical Properties of Fibers (USCS system of units)

## Slide 13: Example
Property | Units | Epoxy | Aluminum | Polyamide
Axial modulus Transverse modulus Axial Poisson's ratio Transverse Poisson's ratio Axial shear modulus Coefficient of thermal expansion Coefficient of moisture expansion Axial tensile strength Axial compressive strength Transverse tensile strength Transverse compressive strength Shear strength Specific gravity | Msi Msi - - - - - - Msi μin/in/0F in/in/lb/lb ksi ksi ksi ksi ksi - - - | 0.493 0.493 0.3 0.3 0.1897 35 0.33 10.44 14.79 10.44 14.79 4.93 1.2 | 10.30 10.30 0.30 0.30 3.915 12.78 0.00 40.02 40.02 40.02 40.02 20.01 2.7 | 0.5075 0.5075 0.35 0.35 0.1885 50 0.33 7.83 15.66 7.83 15.66 7.83 1.2
Table 3.4 Typical Properties of Matrices (USCS system of units)

## Slide 14: Example
a)

## Slide 15: Example
Example 3.1
b)

## Slide 16: Example
c)
Example 3.1

## Slide 17: Example
Example 3.1
d)

## Slide 18: Example
Example 3.1
d)

## Slide 19: Example
Example 3.1
d)

## Slide 20: Example
Example 3.1
d)

## Slide 21: Void Content
FIGURE 3.2 Photomicrographs of cross-section of a lamina with voids.

## Slide 22: Void Content

## Slide 23: Void Content

## Slide 24: Void Content

## Slide 25: Example
Example 3.2
A Graphite/Epoxy cuboid specimen with voids has dimensions of , and its mass is Mc. After putting it in a mixture of sulfuric acid and hydrogen peroxide, the remaining graphite fibers have a mass Mf. From independent tests, the density of graphite and epoxy are ρf and ρm , respectively. Find the volume fraction of the voids in terms of a, b, c, Mf , Mc , ρf , ρm.

## Slide 26: Example

## Slide 27: Example

## Slide 28: Example

## Slide 29: Example

## Slide 30: Example
Alternative Solution

## Slide 31: Example
Alternative Solution

## Slide 32: Example
Alternative Solution

## Slide 33: Example
Alternative Solution

## Slide 34: Example
Alternative Solution

## Slide 35: END