## Slide 1: EML 4230 Introduction to Composite Materials
Chapter 3 Micromechanical Analysis of a Lamina
Elastic Moduli of Unidirectional Lamina
Dr. Autar Kaw
Department of Mechanical Engineering
University of South Florida, Tampa, FL 33620
Courtesy of the Textbook
Mechanics of Composite Materials by Kaw

## Slide 2: Elastic Moduli of Unidirectional Lamina
Longitudinal elastic modulus,
Transverse elastic modulus,
Major Poisson’s ratio,
In-plane shear modulus,

## Slide 3: Strength of Materials Approach
FIGURE 3.3
Representative volume element of a unidirectional lamina.
=
=

## Slide 4: Longitudinal Young’s Modulus
FIGURE 3.4
A longitudinal stress applied to the representative volume element to calculate the longitudinal Young’s modulus for a unidirectional lamina.

## Slide 5: Longitudinal Young’s Modulus

## Slide 6: Longitudinal Young’s Modulus

## Slide 7: Ratio of force taken by fiber to composite

## Slide 8: Ratio of force taken by fiber to composite
FIGURE 3.5
Fraction of load of composite carried by fibers as a function of fiber volume fraction for constant fiber to matrix moduli ratio.

## Slide 9: Example – Longitudinal Young’s Modulus
Find the longitudinal elastic modulus of a unidirectional Glass/Epoxy lamina with a 70% fiber volume fraction. Use the properties of glass and epoxy from Tables 3.1 and 3.2, respectively. Also, find the ratio of the load the fibers take to that of the composite.
Ef = 85 GPa
Em = 3.4 GPa

## Slide 10: Force in fiber to composite ratio

## Slide 11: Comparing with experimental results
FIGURE 3.6
Longitudinal Young’s modulus as function of fiber volume fraction and comparison with experimental data points for a typical glass/polyester lamina.

## Slide 12: Transverse Young’s Modulus
FIGURE 3.7
A transverse stress applied to a representative volume element used to calculate transverse Young’s modulus of a unidirectional lamina.

## Slide 13: Transverse Young’s Modulus
+
= +

## Slide 14: Transverse Young’s Modulus
= +

## Slide 15: Example
Example 3.4
Find the transverse Young's modulus of a Glass/Epoxy lamina with a fiber volume fraction of 70%. Use the properties of glass and epoxy from Tables 3.1 and 3.2, respectively.
= 85 GPa
Em = 3.4 GPa

## Slide 16: Transverse Young’s Modulus vs Fiber Volume Fraction
FIGURE 3.8
Transverse Young’s modulus as a function of fiber volume fraction for constant fiber to matrix moduli ratio.

## Slide 17: Transverse Young’s modulus comparison with experimental data
FIGURE 3.10 Theoretical values of transverse Young’s modulus as a function
of fiber volume fraction for a boron/epoxy unidirectional lamina (Ef = 414 GPa, vf = 0.2, Em = 4.14 GPa, vm = 0.35) and comparison with experimental values. Figure (b) zooms figure (a) for fiber volume fraction between 0.45 and 0.75. (Experimental data from Hashin, Z., NASA tech. rep. contract no. NAS1-8818, November 1970.)

## Slide 18: Major Poisson’s ratio,
FIGURE 3.11
A longitudinal stress applied to a representative volume element to calculate Poisson’s ratio of unidirectional lamina.

## Slide 19: Major Poisson’s Ratio Derivation

## Slide 20: Major Poisson’s Ratio

## Slide 21: Major Poisson’s Ratio

## Slide 22: Example
Find the major and minor Poisson's ratio of a Glass/Epoxy lamina with a 70% fiber volume fraction. Use the properties of glass and epoxy from Tables 3.1 and 3.2, respectively.

## Slide 23: Example
E1 = 60.52 GPa
E2 = 10.37 GPa

## Slide 24: In-Plane Shear Modulus
FIGURE 3.12
An in-plane shear stress applied to a representative volume element for finding in-plane shear modulus of a unidirectional lamina.

## Slide 25: In-Plane Shear Modulus

## Slide 26: In-Plane Shear Modulus

## Slide 27: In-Plane Shear Modulus

## Slide 28: Example
Find the in-plane shear modulus of a Glass/Epoxy lamina with a 70% fiber volume fraction. Use properties of glass and epoxy from Tables 3.1 and 3.2, respectively.

## Slide 29: Example

## Slide 30: In-Plane Shear Modulus comparison with experimental data
FIGURE 3.13 Theoretical values of in-plane shear modulus as a function of fiber volume fraction and comparison with experimental values for a unidirectional glass/epoxy lamina (Gf = 30.19 GPa, Gm = 1.83 GPa). Figure (b) zooms figure (a) for fiber volume fraction between 0.45 and 0.75. (Experimental data from Hashin, Z., NASA tech. rep. contract no. NAS1-8818, November 1970.)

## Slide 31: Mechanics of Materials Equations for Elastic Moduli Summary

## Slide 32: Halpin Tsai Equations
Same as MOM equations for E1 and but NOT for E2 and G12

## Slide 33: Transverse Young’s Modulus
The term ξ is called the reinforcing factor and depends on the following
Fiber Geometry
Packing Geometry
Loading Conditions
Example: For a fiber geometry of circular fibers in a packing geometry of a square array, ξ = 2

## Slide 34: Does have meaning?
Ef/Em = 1 implies = 0, (homogeneous medium)
Ef/Em implies = 1, (rigid inclusions)
Ef/Em implies (voids)

## Slide 35: What is 𝜉 for another case?
For a rectangular fiber cross-section of length a and width b in a hexagonal array,
= 2(a/b),
where a is in the direction of loading.
The term ξ is depends on
Fiber Geometry
Packing Geometry
Loading Conditions

## Slide 36: Example: Transverse Young’s Modulus
Find the transverse Young's modulus for a Glass/Epoxy lamina with a 70% fiber volume fraction. Use the properties for glass and epoxy from Tables 3.1 and 3.2, respectively. Use Halpin-Tsai equations for a circular fiber in a square array packing geometry.
Ef = 85 GPa
Em = 3.4 GPa

## Slide 37: Transverse Young’s Modulus MOM vs HT
FIGURE 3.15 Theoretical values of transverse Young’s modulus as a function of fiber volume fraction and comparison with experimental values for boron/epoxy unidirectional lamina (Ef = 414 GPa, νf = 0.2, Em = 4.14 GPa, νm = 0.35). Figure (b) zooms figure (a) for fiber volume fraction between 0.45 and 0.75. (Experimental data from Hashin, Z., NASA tech. rep. contract no. NAS1-8818, November 1970.)

## Slide 38: In-plane Shear Modulus
The term ξ is called the reinforcing factor and depends on the following
Fiber Geometry
Packing Geometry
Loading Conditions
Example: For a fiber geometry of circular fibers in a packing geometry of a square array, ξ = 1

## Slide 39: What is 𝜉 for another case?
For a rectangular fiber cross-section of length a and width b in a hexagonal array,
,
where is in the direction of loading
The term ξ is depends on
Fiber Geometry
Packing Geometry
Loading Conditions

## Slide 40: Example: In-Plane Shear Modulus
Using Halpin-Tsai equations, find the shear modulus of a Glass/Epoxy composite with a 70% fiber volume fraction. Use the properties of glass and epoxy from Tables 3.1 and 3.2, respectively. Assume the fibers are circular and are packed in a square array.

## Slide 41: Shear Modulus MOM vs HT
Theoretical values of in-plane shear modulus as a function of fiber volume fraction compared with experimental values for unidirectional glass/epoxy lamina (Gf = 30.19 GPa, Gm = 1.83 GPa). Figure (b) zooms figure (a) for fiber volume fraction between 0.45 and 0.75. (Experimental data from Hashin, Z., NASA tech. rep. contract No. NAS1-8818, November 1970.)

## Slide 42: END