## Slide 1: EML 4230 Introduction to Composite Materials
Chapter 3 Micromechanical Analysis of a Lamina
Ultimate Strengths of a Unidirectional Lamina
Dr. Autar Kaw
Department of Mechanical Engineering
University of South Florida, Tampa, FL 33620
Courtesy of the Textbook
Mechanics of Composite Materials by Kaw

## Slide 2: Longitudinal Tensile Strength of Unidirectional Lamina,

## Slide 3: Longitudinal Tensile Strength
Stress–strain curve for a unidirectional composite under uniaxial tensile load along fibers.

## Slide 4: Longitudinal Tensile Strength

## Slide 5: Minimum Fiber Volume Fraction

## Slide 6: Critical Fiber Volume Fraction

## Slide 7: Example, Ultimate Longitudinal Tensile Strength
Find the ultimate longitudinal tensile strength for a Glass/Epoxy lamina with a 70% fiber volume fraction. Use the properties for glass and epoxy from Tables 3.1 and 3.2, respectively. Also, find the minimum and critical fiber volume fractions.

## Slide 8: Example, Minimum Fiber Volume Fraction

## Slide 9: Example, Critical Fiber Volume Fraction

## Slide 10: Experimental Longitudinal Tensile Strength Setup
Tensile coupon mounted in the test frame for finding the tensile strengths of a unidirectional lamina. (Photo courtesy of Dr. R.Y. Kim, University of Dayton Research Institute, Dayton, OH.)

## Slide 11: Coupon Used for Longitudinal Tensile Strength
FIGURE 3.26
Geometry of a longitudinal tensile strength specimen.

## Slide 12: Experimental Results of Longitudinal Tensile Strength
Stress–strain curve for a [0]8 laminate under a longitudinal tensile load. (Data courtesy of Dr. R.Y. Kim, University of Dayton Research Institute, Dayton, OH).

## Slide 13: Video of ASTM D3039 Test

## Slide 14: Modes of Failure under Longitudinal Tensile Stress
Modes of failure of unidirectional lamina under a longitudinal tensile load.

## Slide 15: Longitudinal Compressive Strength of Unidirectional Lamina,

## Slide 16: Longitudinal Compressive Strength
Modes of failure of a unidirectional lamina under a longitudinal compressive load.
Fiber microbuckling extensional mode Fiber microbuckling shear mode
Transverse tensile failure of matrix mode Shear failure mode

## Slide 17: Longitudinal Compressive Strength Transverse Matrix Failure Mode
(Maximum strain failure theory)
(Mechanics of materials formula)
(Empirical Formula)

## Slide 18: Longitudinal Compressive Strength Shear/Extensional Fiber Microbuckling Load
Extensional
Shear

## Slide 19: Longitudinal Compressive Strength Shear Failure Mode

## Slide 20: Longitudinal Compressive Strength
Comparison of experimental and predicted values of longitudinal compressive
strength of unidirectional laminae, Vf =0.50. (Source: Table 7.2 in Introduction to Composite Materials by D. Hull, 1981, 8 Cambridge University Press, 1981, Reprinted with the permission of Cambridge University Press)

## Slide 21: Why experimental numbers do not match theoretical results
Irregular spacing of fibers causing premature failure in matrix-rich areas
Less than perfect bonding between the fibers and the matrix
Poor alignment of fibers
Not accounting for Poisson’s ratio mismatch between the fiber and the matrix
Not accounting for the transversely isotropic nature of fibers such as aramids and graphite

## Slide 22: Example, Longitudinal Compressive Strength
Find the longitudinal compressive strength of a Glass/Epoxy lamina with a 70% fiber volume fraction. Use the properties of glass and epoxy from Tables 3.1 and 3.2, respectively. Assume fibers are circular and are in a square array.

## Slide 23: Using transverse matrix failure

## Slide 24: Using transverse matrix failure

## Slide 25: Using transverse matrix failure

## Slide 26: Example

## Slide 27: Using extensional microbuckling mode
Extensional

## Slide 28: Using shear microbuckling mode
Example 3.14.
Shear

## Slide 29: From Shear Mode Failure
=min(521.8, 4360, 69.4)=69.4 MPa

## Slide 30: Experimental Setup Longitudinal Compressive Strength
Example 3.14.
IITRI fixture mounted in a test frame for finding the compressive strengths of a lamina. (Data reprinted with permission from Experimental Characterization of Advanced Composites, Carlsson, L.A. and Pipes, R.B., Technomic Publishing Co., Inc., 1987, p. 76. Copyright CRC Press, Boca
Raton, FL.)

## Slide 31: Laminate Stacking Sequence
Geometry of a longitudinal compressive strength specimen. (Data reprinted with permission from Experimental Characterization of Advanced Composites, Carlsson, L.A. and Pipes, R.B., Technomic Publishing Co., Inc., 1987, p. 76. Copyright CRC Press, Boca Raton, FL.)

## Slide 32: Experimental Data for Longitudinal Compressive Strength
Stress–strain curve for a [0]24 graphite/epoxy laminate under a longitudinal compressive load. (Data courtesy of Dr. R.Y. Kim, University of Dayton Research Institute, Dayton, OH.)

## Slide 33: Transverse Tensile Strength
FIGURE 3.33
Representative volume element to calculate transverse tensile strength of a unidirectional lamina.

## Slide 34: Transverse Tensile Strength

## Slide 35: Transverse Tensile Strength

## Slide 36: Example
Example 3.15
Find the ultimate transverse tensile strength for a unidirectional Glass/Epoxy lamina with a 70% fiber volume fraction. Use properties of glass and epoxy from Table 3.1 and Table 3.2, respectively. Assume the fibers are circular and are arranged in a square array.

## Slide 37: Example
Example 3.15

## Slide 38: Example
Example 3.15

## Slide 39: Transverse Tensile Strength
Example 3.15
FIGURE 3.34
Stress–strain curve for a [90]16 graphite/epoxy laminate under a transverse tensile load. (Data courtesy of Dr. R.Y. Kim, University of Dayton Research Institute, Dayton, OH.)

## Slide 40: Transverse Compressive Strength

## Slide 41: Example
Example 3.16
Find the ultimate transverse compressive strength of a Glass/Epoxy lamina with 70% fiber volume fraction. Use the properties of glass and epoxy from Table 3.1 and Table 3.2, respectively. Assume the fibers are circular and are packed in a square array.

## Slide 42: Example
Example 3.16

## Slide 43: Example
Example 3.16

## Slide 44: Example
Example 3.16

## Slide 45: Example
Example 3.16

## Slide 46: Example
Example 3.16
FIGURE 3.35
Stress–strain curve for a [90]40 graphite/epoxy laminate under a transverse compressive load perpendicular to the fibers.

## Slide 47: Example
Example 3.16

## Slide 48: In-Plane Shear Strength

## Slide 49: In-Plane Shear Strength

## Slide 50: Example
Example 3.17
Find the ultimate shear strength for a Glass/Epoxy lamina with 70% fiber volume fraction. Use properties for glass and epoxy from Tables 3.1 and 3.2, respectively. Assume the fibers are circular and are arranged in a square array.

## Slide 51: Example
Example 3.17

## Slide 52: Example
Example 3.17

## Slide 53: Example
Example 3.17
FIGURE 3.36
Schematic of a [±45]2S laminate shear test.

## Slide 54: Example
Example 3.17

## Slide 55: Example
Example 3.17

## Slide 56: Example
Example 3.17

## Slide 57: Example
Example 3.17
FIGURE 3.37
Shear stress–shear strain curve obtained from a [±45]2S graphite/epoxy laminate under a tensile load.

## Slide 58: END