## Slide 1: EML 4230 Introduction to Composite Materials
Chapter 4 Macromechanical Analysis of a Laminate
Relating Loads to Midplane Strains/Curvatures
Dr. Autar Kaw
Department of Mechanical Engineering
University of South Florida, Tampa, FL 33620
Courtesy of the Textbook
Mechanics of Composite Materials by Kaw

## Slide 2: Laminate Stacking Sequence
FIGURE 4.1
Schematic of a lamina

## Slide 3: Types of loads allowed in CLT analysis
Nx = normal force resultant in the x direction (per unit length)
Ny = normal force resultant in the y direction (per unit length)
Nxy = shear force resultant (per unit length)
FIGURE 4.3
Resultant forces and moments on a laminate.

## Slide 4: Types of loads allowed in CLT analysis
Mx = bending moment resultant in the yz plane (per unit length)
My = bending moment resultant in the xz plane (per unit length)
Mxy = twisting moment resultant (per unit length)

## Slide 5: Stacking Sequence
FIGURE 4.6
Coordinate locations of plies in the laminate.

## Slide 6: Stresses in a Lamina in a Laminate

## Slide 7: Forces and Stresses

## Slide 8: Forces & Midplane Strains/Curvatures

## Slide 9: Forces & Midplane Strains/Curvatures

## Slide 10: Integrating terms

## Slide 11: Forces & Midplane Strains/Curvatures

## Slide 12: Stiffness Matrices
[A] – Extensional stiffness matrix relating the resultant in-plane forces to the in-plane strains.
[B] – Coupling stiffness matrix coupling the force and moment terms to the midplane strains and midplane curvatures.

## Slide 13: Stresses in a Lamina in a Laminate

## Slide 14: Moments and Stresses

## Slide 15: Moments & Midplane Strains/Curvatures

## Slide 16
Moments & Midplane Strains/Curvatures

## Slide 17
Moments & Midplane Strains/Curvatures

## Slide 18: Stiffness Matrices
[A] – Extensional stiffness matrix relating the resultant in-plane forces to the in-plane strains.
[B] – Coupling stiffness matrix coupling the force and moment terms to the midplane strains and midplane curvatures.
[D] – Bending stiffness matrix relating the resultant bending moments to the plate curvatures.

## Slide 19: Forces, Moments, Midplane Strains, Midplane Curvatures

## Slide 20: END