## Slide 1: EML 4230 Introduction to Composite Materials
Chapter 4 Macromechanical Analysis of a Laminate
Laminate Analysis: Example
Dr. Autar Kaw
Department of Mechanical Engineering
University of South Florida, Tampa, FL 33620
Courtesy of the Textbook
Mechanics of Composite Materials by Kaw

## Slide 2: Laminate Stacking Sequence
Schematic of a laminate

## Slide 3: Problem
A [0/30/-45] Graphite/Epoxy laminate is subjected to a load of Nx = Ny = 1000 N/m. Use the unidirectional properties from Table 2.1 of Graphite/Epoxy. Assume each lamina has a thickness of 5 mm. Find
the three stiffness matrices [A], [B] and [D] for a three ply [0/30/-45] Graphite/Epoxy laminate.
mid-plane strains and curvatures.
global and local stresses on top surface of 300 ply.
percentage of load Nx taken by each ply.
Thickness and coordinate locations of the three-ply laminate.

## Slide 4: Calculating stiffness matrices
A) The reduced stiffness matrix for the 0 Graphite/Epoxy ply is

## Slide 5
Qbar Matrices for Laminas

## Slide 6
The total thickness of the laminate is
h = (0.005)(3) = 0.015 m.
h0=-0.0075 m
h1=-0.0025 m
h2=0.0025 m
h3=0.0075 m
Coordinates of top & bottom of plies
Thickness and coordinate locations of the three-ply laminate.

## Slide 7: Calculating [A] matrix

## Slide 8: The [A] matrix

## Slide 9: Calculating the [B] Matrix

## Slide 10: The [B] Matrix

## Slide 11: Calculating the [D] matrix

## Slide 12: The [D] matrix

## Slide 13: All three stiffness matrices together

## Slide 14: B) Since the applied load is Nx = Ny = 1000 N/m, the mid-plane strains and curvatures can be found by solving the following set of simultaneous linear equations
Setting up the 6x6 matrix

## Slide 15: Mid-plane strains and curvatures

## Slide 16: C) The strains and stresses at the top surface of the 300 ply are found as follows. The top surface of the 300 ply is located at z = h1 = -0.0025 m.
Global strains at top of 30o ply
Thickness and coordinate locations of the three-ply laminate.

## Slide 17: Global strains (m/m)
Ply # | Position | εx | εy | 
1 (00) | Top Middle Bottom | 8.944 (10-8) 1.637 (10-7) 2.380 (10-7) | 5.955 (10-6) 5.134 (10-6) 4.313 (10-6) | -3.836 (10-6) -2.811 (10-6) -1.785 (10-6)
2 (300) | Top Middle Bottom | 2.380 (10-7) 3.123 (10-7) 3.866 (10-7) | 4.313 (10-6) 3.492 (10-6) 2.670 (10-6) | -1.785 (10-6) -7.598 (10-7) 2.655 (10-7)
3(-450) | Top Middle Bottom | 3.866 (10-7) 4.609 (10-7) 5.352 (10-7) | 2.670 (10-6) 1.849 (10-6) 1.028 (10-6) | 2.655 (10-7) 1.291 (10-6) 2.316 (10-6)

## Slide 18
Global stresses in 30o ply at top

## Slide 19: Global stresses (Pa)
Ply # | Position | σx | σy | τxy
1 (00) | Top Middle Bottom | 3.351 (104) 4.464 (104) 5.577 (104) | 6.188 (104) 5.359 (104) 4.531 (104) | -2.750 (104) -2.015 (104) -1.280 (104)
2 (300) | Top Middle Bottom | 6.930 (104) 1.063 (105) 1.434 (105) | 7.391 (104) 7.747 (104) 8.102 (104) | 3.381 (104) 5.903 (104) 8.426 (104)
3 (-450) | Top Middle Bottom | 1.235 (105) 4.903 (104) -2.547 (104) | 1.563 (105) 6.894 (104) -1.840 (104) | -1.187 (105) -3.888 (104) 4.091 (104)

## Slide 20: The local strains and local stress as in the 300 ply at the top surface
Local Strains at top of 30o ply

## Slide 21: Local strains (m/m)
Ply # | Position | ε1 | ε2 | γ12
1 (00) | Top Middle Bottom | 8.944 (10-8) 1.637 (10-7) 2.380 (10-7) | 5.955(10-6) 5.134(10-6) 4.313(10-6) | -3.836(10-6) -2.811(10-6) -1.785(10-6)
2 (300) | Top Middle Bottom | 4.837(10-7) 7.781(10-7) 1.073(10-6) | 4.067(10-6) 3.026(10-6) 1.985(10-6) | 2.636(10-6) 2.374(10-6) 2.111(10-6)
3 (-450) | Top Middle Bottom | 1.396(10-6) 5.096(10-7) -3.766(10-7) | 1.661(10-6) 1.800(10-6) 1.940(10-6) | -2.284(10-6) -1.388(10-6) -4.928(10-7)

## Slide 22
Local stresses in top of 30o ply

## Slide 23: Local stresses (Pa)
Ply # | Position | σ1 | σ2 | 12
1 (00) | Top Middle Bottom | 3.351 (104) 4.464 (104) 5.577 (104) | 6.188 (104) 5.359(104) 4.531 (104) | -2.750 (104) -2.015 (104) -1.280 (104)
2 (300) | Top Middle Bottom | 9.973 (104) 1.502 (105) 2.007 (105) | 4.348 (104) 3.356 (104) 2.364 (104) | 1.890 (104) 1.702 (104) 1.513 (104)
3 (-450) | Top Middle Bottom | 2.586 (105) 9.786 (104) -6.285 (104) | 2.123 (104) 2.010 (104) 1.898 (104) | -1.638 (104) -9.954 (103) -3.533 (103)
Ply # | Position | σ1 | σ2 | 
1 (00) | Top Middle Bottom | 3.351 (104) 4.464 (104) 5.577 (104) | 6.188 (104) 5.359(104) 4.531 (104) | -2.750 (104) -2.015 (104) -1.280 (104)
2 (300) | Top Middle Bottom | 9.973 (104) 1.502 (105) 2.007 (105) | 4.348 (104) 3.356 (104) 2.364 (104) | 1.890 (104) 1.702 (104) 1.513 (104)
3 (-450) | Top Middle Bottom | 2.586 (105) 9.786 (104) -6.285 (104) | 2.123 (104) 2.010 (104) 1.898 (104) | -1.638 (104) -9.954 (103) -3.533 (103)

## Slide 24: D) Portion of load taken by each ply
Portion of load Nx taken by 00 ply = 4.464(104)(5)(10-3) = 223.2 N/m
Portion of load Nx taken by 300 ply = 1.063(105)(5)(10-3) = 531.5 N/m
Portion of load Nx taken by -450 ply = 4.903(104)(5)(10-3) = 245.2 N/m
The sum total of the loads shared by each ply is 1000 N/m, (223.2 + 531.5 + 245.2) which is the applied load in the x-direction, Nx.
Thickness and coordinate locations of the three-ply laminate.
Portion of load taken by each ply

## Slide 25
Percentage of load Nx taken by 00 ply
Percentage of load Nx taken by 300 ply
Percentage of load Nx taken by -450 ply

## Slide 26: END