## Slide 1: EML 4230 Introduction to Composite Materials
Chapter 3 Micromechanical Analysis of a Lamina
Ultimate Strengths of a Unidirectional Lamina
Part 2
Dr. Autar Kaw
Department of Mechanical Engineering
University of South Florida, Tampa, FL 33620
Courtesy of the Textbook
Mechanics of Composite Materials by Kaw

## Slide 2: Transverse Compressive Strength of Unidirectional Lamina,

## Slide 3: Derivation for Transverse Compressive Strength
Remember for the transverse tensile strength formula derivation
Following same logic

## Slide 4: Example, Transverse Compressive Strength
Find the ultimate transverse compressive strength of a Glass/Epoxy lamina with 70% fiber volume fraction. Use the properties of glass and epoxy from Table 3.1 and Table 3.2, respectively. Assume the fibers are circular and are packed in a square array.

## Slide 5: Example, Transverse Compressive Strength

## Slide 6: Experimental Results for Transverse Compressive Strength Test
FIGURE 3.35
Stress–strain curve for a [90]40 graphite/epoxy laminate under a transverse compressive load perpendicular to the fibers.

## Slide 7: In-Plane Shear Strength of Unidirectional Lamina,

## Slide 8: Derivation In-Plane Shear Strength

## Slide 9: Derivation of In-Plane Shear Strength

## Slide 10: Example, In-Plane Shear Strength
Find the ultimate shear strength for a Glass/Epoxy lamina with 70% fiber volume fraction. Use properties for glass and epoxy from Tables 3.1 and 3.2, respectively. Assume the fibers are circular and are arranged in a square array.

## Slide 11: In-Plane Shear Strength Test
Schematic of a [±45]2S laminate shear test.

## Slide 12: Experimental Results for In-Plane Shear Strength Test
Shear stress–shear strain curve obtained from a [±45]2S graphite/epoxy laminate under a tensile load.

## Slide 13: END